RAINTRADE CORPORATION

19 SKOKIE VALLEY RD.
LAKE BLUFF, IL 60044

# COPPER ROOFING COIL AND SHEET SPECIFICATIONS

## Mechanical Properties

TENSILE		36.0 KSI

YIELD			28.0 KSI

ELONGATION	30%2”

ROCKWELL		F 60

## Nominal Chemical Composition

CDA ALLOY			DESCRIPTION		Cu

110				Copper Roofing Coil 		99.9

## Alloy

ETP 110 Copper Coil to ASTM B 370

## Hardness

1/8  -  ¼  Hard

This is to certify that this material was manufactured pursuant to the requirements of the above composition/specification.

This material was manufactured and stored in mercury free condition.

This certificate is an advisory only and is not a warranty.  This material is warranted as set forth in the Manufacturer’s Standard Warranty.